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	Product characteristics

	(text highlighted in red can be deleted depending on your choice)

	

	Description

	Loggialu® Paro 0140 Privacy combines the functionality of an efficient sun protection panel with an elegant appearance and aesthetic design in a high quality contemporary concept.

	With the Privacy concept the blades are moveable, as such the blades can be manually tilted from closed to fully open or vice versa.

	The sturdy circumferential frame of extruded aluminium, guarantees a good dimensional stability as a whole, without any visible corner joints.

	

	Standards

	Aluminium-Alloy Al Mg Si 0.5 (F25):

	 - Standard: EN AW-6063

	 - Curing: T66

	Aluminium pre-treatment:

	 - Standard DIN 5002155

	Strength calculations are based on the following standards:

	 - ENV 1999-1-1: Calculations of aluminium constructions

	 - NBN B-03-002-2: Wind load - Dynamic effects

	 - EN 1991-1-4: Wind load

	Panel meets all CE requirements as stated in the declaration of performance DoP/RP/001 on the basis of harmonised technical specifications according to EN 13659:2004.

	

	Surface treatment - aluminium

	Natural colour anodised F1 (20 µm): pre-treated and anodized.

	Polyester powder coating in RAL-colours (60-80 µm): aluminium profiles corrosion resistance pre-treated (DIN 5002155) to guarantee a firm powder coating after which thermally painted.

	

	System execution

	Frame:

	 - Vertical frame profiles LG.040.07, laterally provided with a finishing profile LG.040.08 for level view, made from extruded aluminium

	●  Dimensions of the frame profile:

	    - Width: 40 mm

	    - Depth: 40 mm

	    - Minimum inertia moments Iy = 94,248 mm4 (strong axis); Iz = 67,516 mm4, where a minimal material thickness of 2.0 mm

	 - Depending on the height of the sliding panel the horizontal frame profile can measure 55 mm high at the top instead of 40 mm and 70 mm below instead of 40 mm

	●  Horizontal frame profile LG.040.09:

	    - Depth: 40 mm

	    - Height: 40 mm

	    - Minimum inertia moments Iy = 75,158 mm4 (strong axis); Iz = 72,301 mm4, where a minimal material thickness of 2.0 mm

	●  Horizontal frame profile LG.040.55:

	    - Depth: 40 mm

	    - Height: 55 mm

	    - Minimum inertia moments Iy = 169,579 mm4 (strong axis); Iz = 91,248 mm4, where a minimal material thickness of 2.0 mm

	●  Horizontal frame profile LG.040.70:

	    - Depth: 40 mm

	    - Height: 70 mm

	    - Minimum inertia moments Iy = 317,123 mm4 (strong axis); Iz = 116,033 mm4, where a minimal material thickness of 2.0 mm

	 - Invisible corner joints by means of finishing profile and end caps

	Blades:

	 - Parallelogram shaped aluminium blades ICR.066.01, suitable for manual tilting from a closed to open position or vice versa with two control settings, which allows for one section to be closed and the other open

	●  Dimensions:

	    - Height: 16 mm

	    - Depth: 65 mm

	    - Blade pitch: 57 mm (17 blades at 1 meter high)

	    - Minimum inertia moments Iy = 75,983 mm4 (strong axis); Iz = 6,786 mm4, where a minimal material thickness of 1.5 mm

	Slide fittings:

	 - High quality maintenance free sliding fittings, comprise of:

	    - sliding rail (above) with trolley / suspension bracket and adjustable railstop or with rear rails

	    - guiding system (under) aluminium L-profile 20/20/4 and plastic guiding system 

	    - lateral rubberstop to prevent damage to the panel 

	 - Movement capabilities of the sliding panel (according to chosen design): simple - or symmetrical sliding

	 - Motorised control - according to chosen design

	 - 230 V motor - for connection to simple switch or buildings control system

	 - Slide fittings CE approved

	System properties:

	 - Blades manually tilt, from closed position to fully open or vice versa in two control settings

	 - Frame profile with level view and invisible inner corner joints

	 - Depending on the height of the sliding panel the horizontal frame profile can measure 55 mm high at the top instead of 40 mm and 70 mm below instead of 40 mm

	Dimensions:

	 - Maximum possible dimensions depend on local wind load qb

	Optional accessories:

	 - Flexible under guiding system Flexguide®: self-regulating under guiding system for sloping areas with L-, T of U-shaped (incorporated) under guiding systems profile - see separate specification sheet



